## Slide 1
1
Biomedical Polymers
PRESENTED BY
Abbas Al-Bawee

## Slide 2: CONTENTS
Introduction
Classification
Selection parameters for biomedical polymers
Applications
Conclusion
2

## Slide 4: obtained
compound
from
Macromolecular natural origin.
Chemical nature - polysaccharides, protein and bacterial polyesters.

## Slide 5: Properties Of Biomedical Polymers
Flexibility;
Resistance to biochemical attack;
Good biocompatibility;
Light weight;
Available in a wide variety of compositions with adequate physical and mechanical properties and
Can be easily manufactured into products with the desired shape.

## Slide 6: Classification
Biomedical Polymers
Natural Polymers
Synthetic Polymers

## Slide 7: Natural polymers
Natural polymers, or polymers, derived from living
creatures, are of great interest in the biomaterials field.
Properties of natural polymers:
Biodegradable;
Non-toxic/ non-inflammatory;
Mechanically similar to the tissue to be replaced;
Highly porous;
ABBAS- -14 0ALBAWEE
2021-026:26:18
--------------------------------------------
مواد قابلة للتحلل

## Slide 8
Encouraging of cell attachments and growth;
Easy and cheap to manufacture
Capable of attachment with other molecules
(to potentially increase scaffold interaction with normal tissue).
ABBAS- ALBAWEE
2021-02-14 06:35:32
--------------------------------------------
خلايا هذا المواد قابلة للنمو والتأقلم مع الانسجة الحية

## Slide 9: Example of natural polymers
Collagen
Cellulose
Alginates
Dextrans and
Chitosan
ABBAS- ALBAWEE
2021-02-14 06:38:21
--------------------------------------------
الجينات

## Slide 10: Collagen
Consist of three intertwined protein chains, helical structure
Collagen…..non-toxic, minimal immune response
Can be processed into a variety formats
  Porous sponges,Gels, and Sheets
Applications
  Surgery, Drug delivery, Prosthetic implants and tissue-engineering of multiple organs
ABBAS- ALBAWEE
2021-02-14 06:40:39
--------------------------------------------
هيكل حلزوني
ABBAS- ALBAWEE
2021-02-14 06:42:54
--------------------------------------------
لديه الحد الأدنى من الاستجابة المناعية
ABBAS- ALBAWEE
2021-02-14 06:43:59
--------------------------------------------
الاطراف الاصطناعية

## Slide 11: Chitosan
Derived from chitin, present in hard exoskeletons of shellfish like shrimp and crab
Chitosan desirable properties
Minimal foreign body reaction
mechanical biodegradation
Controllable properties
Applications
In the engineering of cartilage, nerve, and liver tissue,
wound dressing and drug delivery devices
ABBAS- ALBAWEE
2021-02-14 21:02:03
--------------------------------------------
كياتين
ABBAS- ALBAWEE
2021-02-14 21:03:17
--------------------------------------------
هياكل خارجية
ABBAS- ALBAWEE
2021-02-14 22:58:23
--------------------------------------------
موجود في المحار والجمبري
ABBAS- ALBAWEE
2021-02-14 23:01:49
--------------------------------------------
اقل تفاعل مع الاجسام الغريبة الخارجية اي انه لايتاثر بسهولة
ABBAS- ALBAWEE
2021-02-14 23:07:02
--------------------------------------------
يمكن التحكم او السيطرة عليها
ABBAS- ALBAWEE
2021-02-14 23:10:54
--------------------------------------------
من ناحية الخصائص الميكانيكية او التحليل البايلوجي
ABBAS- ALBAWEE
2021-02-14 23:11:53
--------------------------------------------
الغضاريف والأعصاب والكبد

## Slide 12: Alginate
A polysaccharide derived from brown seaweed
Can be processed easily in water
Non-toxic
Biodegradable
Controllable porosity
  Forms a solid gel under mild processing conditions
Applications in
Liver, nerve, heart, cartilage & tissue- engineering
12
ABBAS- ALBAWEE
2021-02-14 23:16:56
--------------------------------------------
بولي سكاريد
ABBAS- ALBAWEE
2021-02-14 23:39:21
--------------------------------------------
قابل للتحلل
ABBAS- ALBAWEE
2021-02-14 23:40:02
--------------------------------------------
يمكن السيطرة على مساميتها

## Slide 13: Synthetic Polymers
Advantages of Synthetic Polymers
Ease of manufacturability
process ability
reasonable cost
The Required Properties
Biocompatibility
Sterilizability
Physical Property
Manufacturability
ABBAS- ALBAWEE
2021-02-14 23:52:17
--------------------------------------------
تكلفة معقولة
ABBAS- ALBAWEE
2021-02-14 23:53:54
--------------------------------------------
تعقيم
ABBAS- ALBAWEE
2021-02-14 23:54:23
--------------------------------------------
توافق حيوي
ABBAS- ALBAWEE
2021-02-14 23:54:51
--------------------------------------------
قابلية التصنيع

## Slide 14
Applications:
Medical disposable supplies, Prosthetic materials, Dental materials, implants, dressings, polymeric drug delivery, tissue engineering products
ABBAS- ALBAWEE
2021-02-15 06:52:12
--------------------------------------------
اللوازم والامدادات الطبية
ABBAS- ALBAWEE
2021-02-15 06:53:18
--------------------------------------------
المواد التعويضية او المواد التي تستخدم في الاطراف الاصطناعية

## Slide 15: Synthetic Polymers
Example of Synthetic Polymers :
(PTFE) Polytetrafluoroethylene
Polyethylene, (PE)
Polypropylene, (PP)
Poly (methyl methacrylate), PMMA
Materials in Maxillofacial Prosthetic
ABBAS- ALBAWEE
2021-02-15 06:56:15
--------------------------------------------
المواد المستخدمة في استبدال الوجه والفكين

## Slide 16: Classification of synthetic polymers
Synthetic Polymers
Biostable
Bioerodible
Water
soluble
Other
polymers

## Slide 17: Biostable Polymers
Polymers that are sufficiently biostable to allow their long term use in artificial organs blood pumps, blood vessel prostheses, heart valves, skeletal joints, kidney prostheses.
A polymer must fulfill certain critical requirements if it is to be used in an artificial organ.
It must be physiologically inert
The polymer itself should be stable during many years of exposure to hydrolytic or oxidative conditions at body temperature
ABBAS- ALBAWEE
2021-02-15 07:06:46
--------------------------------------------
المفاصل الهيكلية
ABBAS- ALBAWEE
2021-02-15 07:09:17
--------------------------------------------
يجب ان تلبي المتطلبات الهامة والحرجة
ABBAS- ALBAWEE
2021-02-15 07:10:15
--------------------------------------------
تكون خاملة من الناحية الفسيولوجية
ABBAS- ALBAWEE
2021-02-15 07:11:56
--------------------------------------------
متحلل بالماء او الاكسدة

## Slide 18
It must be strong and resistant to impact (when it is used as structural material to replace the bone).
The polymer must be sufficiently stable chemically or thermally that it can be sterilized by chemicals or by heat.

## Slide 19: Bioerodible Polymers
Polymers that are bioerodible materials that will serve a short term purpose in the body and then
decompose metabolized
to small molecules that or excreted, sometimes
can be
with the
concurrent release of drug molecules.
Mostly bioerodible polymers used as surgical sutures, tissue in growth materials, or controlled release of drug.
ABBAS- ALBAWEE
2021-02-15 07:17:53
--------------------------------------------
العمليات الايضية داخل الجسم
ABBAS- ALBAWEE
2021-02-15 07:18:17
--------------------------------------------
الفرز
ABBAS- ALBAWEE
2021-02-15 07:19:28
--------------------------------------------
عموما
ABBAS- ALBAWEE
2021-02-15 07:20:47
--------------------------------------------
الغرز

## Slide 20: Water Soluble Polymers
Water-soluble polymers (usually bioerodible) that form part of plasma or whole blood substitute solutions or which function as macromolecular drugs.
Applications:
Improvement in the behavior of pharmaceuticals.
Used in synthetic blood substitutes as viscosity enhancers or as oxygen-transport macromolecules.
ABBAS- ALBAWEE
2021-02-15 07:24:13
--------------------------------------------
سلوك المستحضرات الصيدلانية.

## Slide 21: Selection Parameters For Biomedical Polymers
The design and selection of biomaterials depend on different properties –
Host Response
Biocompatibility
Biofunctionality
Functional Tissue Structure and Pathobiology
Toxicology
Appropriate Design and Manufacturability
Mechanical Properties of Biomedical p2o1 lymers
ABBAS- ALBAWEE
2021-02-19 06:17:27
--------------------------------------------
استجابة الجسم المضيف
ABBAS- ALBAWEE
2021-02-19 06:18:23
--------------------------------------------
Ø التوافق الحيوي
ABBAS- ALBAWEE
2021-02-19 06:19:22
--------------------------------------------
Ø الوظيفة الحيوية

## Slide 22
Host Response: The response of the host organism (local and systemic) to the implanted polymeric material or device.
Biocompatibility : The ability of a material to perform with an appropriate host response, in a specific application.
Toxicology: Should not be toxic.
Appropriate Design and Manufacturability:
Biomaterials should be machinable, moldable, extrudable.
Mechanical Properties of Biomedical polymers: Tensile strength, yield strength, elastic modulus, surface finish, creep, and hardness.
22
ABBAS- ALBAWEE
2021-02-15 07:28:49
--------------------------------------------
قابل التشكيل والبثق
ABBAS- ALBAWEE
2021-02-19 06:23:23
--------------------------------------------
يؤدي الغرض

## Slide 23: Application
Cardiovascular Applications Bones, Joints, And Teeth Contact
Lenses And Intraocular Lenses
Artificial Kidney And Hemodialysis Materials Oxygen-Transport Membranes
Surgical Sutures Tissue Ingrowth Polymers
Controlled Release Of Dr2u3 gs
ABBAS- ALBAWEE
2021-02-19 06:24:39
--------------------------------------------
تطبيقات القلب والأوعية الدموية

## Slide 24
Heart Valves and Vascular Prostheses
The Artificial Heart Heart pump designs

## Slide 25
Silicone rubber is used because of its inertness, elasticity, and low capacity to cause blood clotting.
Damaged heart valves, weakened arterial walls, and blocked arteries constitute some of the commonest cardiovascular disorders.
Poly(tetrafluoroethylene)
ABBAS- ALBAWEE
2021-02-19 06:29:56
--------------------------------------------
جدرا الشرايين الضعيفة
ABBAS- ALBAWEE
2021-02-19 06:31:16
--------------------------------------------
الشراييين المسدودة

## Slide 26: Artificial Heart
Artificial hearts are a mechanical device, they are typically used in order to bridge the time to heart transplantation, or to permanently replace the heart in case transplantation is impossible.
ABBAS- ALBAWEE
2021-02-19 06:42:05
--------------------------------------------
تنظيم ضربات القلب او عمل القلب
ABBAS- ALBAWEE
2021-02-19 06:42:41
--------------------------------------------
او ليحل بشكل دائم بدل القلب

## Slide 27: Artificial Heart
The heart is conceptually simple, it’s formed by
materials consequence
and power supplies. A it could be the body
synthetic possible rejection.
These complications limited the
lifespan of early human recipients to hours or days
ABBAS- ALBAWEE
2021-02-19 06:45:26
--------------------------------------------
القلب الصناعي
ABBAS- ALBAWEE
2021-02-19 06:45:55
--------------------------------------------
من الناحية النظرية
ABBAS- ALBAWEE
2021-02-19 06:49:26
--------------------------------------------
ان يرفض الجسم عمل القلب الاصطناعي فهذه نتيجة محتملة
ABBAS- ALBAWEE
2021-02-19 06:51:09
--------------------------------------------
عمر الانسان

## Slide 28: ABIO HEART
It’s the last artificial heart invented. It’s made by titanium and a special plastic in which the blood doesn’t stick. The heart has got flexible walls with silicon, a motor that moves it, and in the valve it controls the pressure.
5 years are the life of this hearts.
ABBAS- ALBAWEE
2021-02-19 22:24:47
--------------------------------------------
يجري الدم فيه بشكل طبيعي جدا

## Slide 29: Heart Pump Designs

## Slide 30: Bones, Joints, And Teeth
Occasionally repaired with the use of polyurethanes, epoxy resins, and rapid curing vinyl resins.
Silicone rubber rods and closed cell sponges- replacement finger and wrist joints.
Elbow joints- vinyl polymers and nylon
Knee joints- cellophane and, more rubber
recently,
silicone
Poly(methyl methacrylate) is the principal polymer used both for acrylic teeth and for the base material
ABBAS- ALBAWEE
2021-02-19 07:19:01
--------------------------------------------
sometimes
ABBAS- ALBAWEE
2021-02-19 07:09:37
--------------------------------------------
مفاصل المرفق
ABBAS- ALBAWEE
2021-02-19 07:10:18
--------------------------------------------
مفصل الركبة
ABBAS- ALBAWEE
2021-02-19 07:12:29
--------------------------------------------
في الاونة الاخيرة السلكون المطاطي

## Slide 31: Contact Lenses And Intraocula Lenses
r
31

## Slide 32: Artificial Kidney And Hemodialysis
clotting-polycarbonate or cellulose acetate fibers.
Materials
The function of a kidney is to remove low molecular
weight waste products from the bloodstream.
Artificial kidneys have function by passage of the blood between the walls of a dialysis cell which is immersed in a circulating fluid.
Cellophane- Semipermeable dialysis membranes
The polymer is "heparinized" to prevent blood
32
ABBAS- ALBAWEE
2021-02-19 07:26:23
--------------------------------------------
الكلى الصناعية وغسيل الكلى
ABBAS- ALBAWEE
2021-02-19 07:28:55
--------------------------------------------
خلية غسل الكلية
ABBAS- ALBAWEE
2021-02-19 07:32:40
--------------------------------------------
أغشية غسيل الكلى شبه المنفذة
ABBAS- ALBAWEE
2021-02-19 07:33:13
--------------------------------------------
مغمورة في سائل معين
ABBAS- ALBAWEE
2021-02-19 07:35:55
--------------------------------------------
يكون معالجا بالهيبارين
ABBAS- ALBAWEE
2021-02-19 07:38:37
--------------------------------------------
ليمنع تخثر الدم من قبل المواد البوليمرية

## Slide 33: Oxygen-Transport Membranes
Surgical work on the heart frequently requires the use of a heart lung machine to circulate and
membranes are highly
oxygenate the blood.
Poly(dimethylsiloxane) efficient gas transporters.
It is of interest that silicons rubber has approximately six times the oxygen permeability of fluorosilicones.
ABBAS- ALBAWEE
2021-02-19 07:39:32
--------------------------------------------
أغشية نقل الأكسجين
ABBAS- ALBAWEE
2021-02-19 07:45:21
--------------------------------------------
ثنائي ميثيل السيلوكزان

## Slide 34
Poly(glycolic acid), or condensation copolymers of glycolic acid with lactic acid.
A high tensile strength and is compatible
The polymer degrades by hydrolysis to nontoxic glycolic acid.

## Slide 35: Drug release by diffusion
Early encapsulation and entrapment systems released the drug from within the polymer via molecular diffusion
When the polymer absorbs water it swells in size
Swelling created voids throughout the interior polymer
Smaller molecule drugs can escape via the voids at a known rate controlled by molecular diffusion (a function of temperature and drug size)
Add wate r
Add
time
ABBAS- ALBAWEE
2021-02-19 22:57:46
--------------------------------------------
ايصال الدواء عن طريق الانتشار
ABBAS- ALBAWEE
2021-02-19 23:14:47
--------------------------------------------
امظمة التغليف
ABBAS- ALBAWEE
2021-02-19 23:16:37
--------------------------------------------
من خلا انتشار جزيئي
ABBAS- ALBAWEE
2021-02-19 23:19:04
--------------------------------------------
هذا التغير او التورم في حجم المادة البوليمرية

## Slide 36: Drug release by erosion
Modern delivery systems employ biodegradable polymers
  When the polymer is exposed to water hydrolysis occurs
  Hydrolysis degrades the large polymers into smaller biocompatible compounds
– Surface erosion process
– Bulk erosion process
mer
mer
mer
mer
Polymer Water attacks
bond
mer mer mer mer mer
mer mer mer mer mer
mer mer
mer
mer
mer mer mer mer mer mer mer mer mer
36
ABBAS- ALBAWEE
2021-02-19 23:34:22
--------------------------------------------
التاكل
ABBAS- ALBAWEE
2021-02-19 23:36:12
--------------------------------------------
التحلل المائي
ABBAS- ALBAWEE
2021-02-19 23:42:29
--------------------------------------------
مركبات متوافقة حيويا
ABBAS- ALBAWEE
2021-02-19 23:46:46
--------------------------------------------
عملية التآكل بالكامل
ABBAS- ALBAWEE
2021-02-19 23:47:11
--------------------------------------------
عملية تآكل السطح

## Slide 37: Bulk erosion
(e.g. poly lactide, polyglycolic acid)
When the polymer is exposed to water hydrolysis
occurs
Hydrolysis degrades the large polymers into smaller biocompatible compounds
These small compound diffuse out of the matrix through the voids caused by swelling
Loss of the small compounds accelerates the formation
of voids thus the exit of drug molecules
Add
time
Add
wate
r

## Slide 38: Surface erosion (e.g., polyanhydrides)
–When the polymer is exposed to water hydrolysis occurs
–Hydrolysis degrades the large polymers into smaller biocompatible compounds
– These small compound diffuse from the interface of the polymer
– Loss of the small compounds reveals drug trapped within
–Note these polymer do not swell.
Add
time
Add
wate
r

## Slide 39
Biomedical polymers are essentially a biomaterial, that is used and adapted for a medical application. Biomedical polymer can have a beginning functional, such as being used for a heart valve and more interactive purpose such as hydroxyapatite coated in implant and such implants are lunching upwards of twenty year. Many prostheses and implants made from polymers have been in use for the last three decades and there is a continuous search for more biocompatible and stronger polymer prosthetic materials.