## Slide 1: Conventional pressing and sintering
After the metallic powders have been produced, the conventional PM sequence consists of three steps:
blending and mixing of the powders;
compaction, in which the powders are pressed into the desired part shape; and
sintering, which involves heating to a temperature below the melting point to cause solid-state bonding of the particles an strengthening of the part.
The three steps, sometimes referred to as primary operations in PM, are portrayed in Figure below.
In addition, secondary operations are sometimes performed to improve dimensional accuracy, increase density, and for other reasons.

## Slide 2: Figure (1): The conventional powder metallurgy production sequence: (1) blending, (2) compacting, and (3) sintering; (a) shows the condition of the particles, whereas (b) shows the operation and/ or workpart during the sequence.

## Slide 3: Blending and mixing of the powders
To achieve successful results in compaction and sintering, the metallic powders must be thoroughly homogenized beforehand.
Blending refers to when powders of the same chemical composition but possibly different particle sizes are intermingled. Different particle sizes are often blended to reduce porosity.
Mixing refers to powders of different chemistries being combined.
An advantage of PM technology is the opportunity to mix various metals into alloys that would be difficult or impossible to produce by other means. The distinction between blending and mixing is not always precise in industrial practice.
Blending and mixing are accomplished by mechanical means. Four alternatives are illustrated in Figure (2): (a) rotation in a drum; (b) rotation in a double-cone container; (c) agitation in a screw mixer; and (d) stirring in a blade mixer.

## Slide 4: Figure (2): Several blending and mixing devices: (a) rotating drum, (b) rotating double-cone, (c) screw mixer, and (d) blade mixer.

## Slide 5
Other ingredients are usually added to the metallic powders during the blending and/ or mixing step.
These additives include:
lubricants, such as stearates of zinc and aluminum, in small amounts to reduce friction between particles and at the die wall during compaction;
binders, which are required in some cases to achieve adequate strength in the pressed but unsintered parts; and;
deflocculants, which inhibit agglomeration of powders for better flow characteristics during subsequent processing.

## Slide 6: Compaction
Methods for compacting of powder materials can be divided to two basic groups:
1. Compaction with the aid of static or dynamic compacting pressure at room or elevated temperature – compacting by single-action or multi-action static compacting pressure in a die with an upper and bottom punch for high-volume manufacturing of parts of various types: forging, isostatic pressing, extrusion pressing, rolling, hot pressing e.g. for draw tools from cemented carbides.
2. Pressureless compaction – free pouring (e.g. a manufacture of filters), jolting, vibration compacting e.g. for fuel elements for nuclear technology and the ceramic casting method.

## Slide 7
Fundamentals of pressing processes
In compaction, high pressure is applied to the powders to form them into the required shape. The conventional compaction method is pressing, in which opposing punches squeeze the powders contained in a die. The steps in the pressing cycle are shown in Figure (3). The workpart after pressing is called a green compact, the word green meaning not yet fully processed.
As a result of pressing, the density of the part, called the green density, is much greater than the starting bulk density. The green strength of the part when pressed is adequate for handling but far less than that achieved after sintering.

## Slide 8
The applied pressure in compaction results initially in repacking of the powders into a more efficient arrangement, eliminating ‘‘bridges’’ formed during filling, reducing pore space, and increasing the number of contacting points between particles.
As pressure increases, the particles are plastically deformed, causing interparticle contact area to increase and additional particles to make contact. This is accompanied by a further reduction in pore volume.
The progression is illustrated in three views in figure (4) for starting particles of spherical shape. Also shown is the associated density represented by the three views as a function of applied pressure.

## Slide 9
Presses used in conventional PM compaction are mechanical, hydraulic, or a combination of the two.A 450 kN (50 ton) hydraulic unit is shown in figure (5).
Because of differences in part complexity and associated pressing requirements, presses can be distinguished as (1) pressing from one direction, referred to as single-action presses; or (2) pressing from two directions, any of several types including opposed ram, double-action, and multiple action.
Current available press technology can provide up to 10 separate action controls to produce parts of significant geometric complexity.

## Slide 10
The capacity of a press for PM production is generally given in tons or kN or MN. The required force for pressing depends on the projected area of the PM part (area in the horizontal plane for a vertical press) multiplied by the pressure needed to compact the given metal powders. Reducing this to equation form
F = Appc
where F = required force, N (lb); Ap = projected area of the part, mm² (in²); and pc = compaction pressure required for the given powder material, MPa (lb/ in²).
Compaction pressures typically range from 70 MPa (10,000 lb/ in²) for aluminum powders to 700 MPa (100,000 lb/ in²) for iron and steel powders.

## Slide 11: Figure (3): Pressing, the conventional method of compacting metal powders in PM: (1) filling the die cavity with powder, done by automatic feed in production, (2) initial, and (3) final positions of upper and lower punches during compaction, and(4) ejection of part.

## Slide 12: Figure (4): (a) Effect of applied pressure during compaction: (1) initial loose powders after filling, (2) repacking, and (3) deformation of particles; and (b) density of the powders as a function of pressure. The sequence here corresponds to steps 1, 2, and 3 in Figure (3).

## Slide 13: Figure (5): A 450-kN (50-ton) hydraulic press for compaction of powder metallurgy components. (Photo courtesy of Dorst America, Inc.)