## Slide 1: Mechanical &Thermal properties of lightweight concrete
BY
Sara M. Nasif & Ghufran A. Abdulkareem
supervision by
Dr. Amr M. Ibrahim

## Slide 2: INTRODUCTION

## Slide 3: CONCRETE 1-cement 2-coarse aggregate 3-sand 4-water

## Slide 4
Lightweight concrete that have density less than 1800kg/m^3
Lightweight concrete
Autoclaved
Aerated concrete
Lightweight aggregate concrete
Foamed concrete

## Slide 5: Lightweight aggregate concrete

## Slide 6: Lightweight aggregate concrete material
Cement
Polystyrene
Water
Insulate
Taksaboon

## Slide 7: the reason of choice polystyrene
1-it have low dead load which lower coast
2- its known as waste material
3-it is a good thermal insulator material
4-it is inner material

## Slide 8: the reason of choice polystyrene
1-it have low dead load which lower coast 2- its known as waste material 3-it is a good thermal insulator material 4-it is inner material

## Slide 9: the stages of project 1-search period 2-processing models 3-test

## Slide 10
Taksaboon mg | Insulate Kg/m^3 | Polystyrene (m^3) | CEMENT (Kg/m^3) | NO. OF MIX
 |  | 1.194 | 420 | 1-
5 | 27 | 1.08 | 380 | 2-
3 | 19 | 1.142 | 390 | 3-
3 | 14 | 1.13 | 380 | 4-
3 | 10 | 1.12 | 400 | 5-
3 | 14 | 1.12 | 461 | 6-

## Slide 13: TEST 1

## Slide 14: TEST 2

## Slide 15
Chart: compressive strength (MPa)& no. of mix
معدل مقاومه الانضغاط MPa | 3.67 | 0.57 | 0.0145 | 2.19 | 3.29 | 4.231


no. of mix | 1 | 2 | 3 | 4 | 5 | 6

## Slide 16
Chart: no. of mix
Chart: density(kg/m^3)&absorbtion (%)
density | 745 | 625 | 420 | 732 | 956 | 1000.2
absorbtion | 15.4 | 12.6 | 11 | 17.24 | 18 | 18.4

## Slide 17
Chart: compressive strength(MPa)&absorbtion (%)
compressive strength | 3.67 | 0.57 | 0.0145 | 2.19 | 3.29 | 4.231
absorbtion | 15.4 | 12.6 | 11 | 17.24 | 18 | 18.4

## Slide 18
Chart: density (kg/m^3) & compressive strength
compressive strength | 3.67 | 0.57 | 0.0145 | 2.19 | 3.29 | 4.231

density | 745 | 625 | 420 | 732 | 956 | 1000.2

## Slide 19
Chart: density&thermal insulator
density | 745 | 625 | 420 | 732 | 956 | 1000.2
thermal insulator | 0.00735 | 0.00821 | 0.009 | 0.00729 | 0.00613 | 0.0056

## Slide 20: conclusions
Density range (420-1002)kg/m^3
Compressive strength range(0.0145-4.231)MPa
Absorption range (11-18.4)%
Insulate<>compressive strength
Insulate have a good thermal isolator