## Slide 1: Highway Materials Lecture - 10
Designed and presented
By
Asst. Prof. Dr. Raquim Nihad Zehawi

## Slide 2
BASIC ENGINEERING PROPERTIES OF SOILS
Phase Relations:
Soils are considered as three-phase systems that consist of air, water, and solids
Schematic of the Three Phases of a Soil Mass
The relative amount of voids in any soil
Porosity (n)
The ratio of the volume of voids to the total volume of the soil
Void Ratio (e)
the ratio of the volume of voids to the volume of solids

## Slide 3
Moisture Content (w)
the ratio of the weight of water Ww in the soil mass to the oven dried weight of solids Ws
Degree of Saturation (S)
the percentage of void space occupied by water

## Slide 4
Density of Soil
The ratio that relates the mass side of the phase diagram to the volumetric side
Total or bulk density
Dry density
Submerged or buoyant density
Total Density
The ratio of the weight of a sample of soil to the volume
The total density for saturated soils
Dry Density
The density of the soil with the water removed
often used to evaluate how well earth embankments have been compacted

## Slide 5
Submerged Density ()
the density of the soil when submerged in water
The specific gravity of soil particles is the ratio of density of the soil particles to the density of distilled water
Specific Gravity of Soil Particles
bulk density can be given as:

## Slide 6
Determining Soil Characteristics Using the Three-Phase Principle
Example 1
Solution:
The wet weight of a specimen of soil is 340 g and the dried weight is 230 g. The volume of the soil before drying is 210 cc. If the specific gravity of the soil particles is 2.75, determine the void ratio, porosity, degree of saturation, and dry density.
weight of the water
For the volume of the water
For the volume of the solids
For the volume of the air

## Slide 7
For the void ratio
For the porosity
For the degree of saturation
For the dry density

## Slide 8
Example 2
Solution:
Determining Soil Characteristics Using the Three-Phase Principle
The moisture content of a specimen of soil is 26 percent, and the bulk density is 116 lb/ft3. If the specific gravity of the soil particles is 2.76, determine the void ratio and the degree of saturation.
The weight of 1 ft3 of the soil is 116 lb—that is

## Slide 10
Atterberg Limits
Atterberg limits: The water content levels at which the soil changes
from one state to the other.
The stiffness or consistency of the soil at any time depends on the state at which the soil is, which in turn depends on the amount of water present in the soil
shrinkage limit (SL)
plastic limit (PL)
liquid limit (LL)

## Slide 11
When a saturated soil is slowly dried, the volume shrinks
shrinkage limit (SL)
The moisture content at which further drying will not result in additional shrinkage is the Shrinkage Limit
plastic limit (PL)
The moisture content at which the soil crumbles when it is rolled down to a diameter of one-eighth of an inch
The moisture content is higher than the PL if the soil can be rolled down to diameters less than one-eighth of an inch

## Slide 12
The moisture content at which the soil will flow and close a groove of one-half inch within it after the standard LL equipment has been dropped 25 times
liquid limit (LL)
Schematic of the Casagrande Liquid Limit Apparatus

## Slide 13
The range of moisture content over which the soil is in the plastic state is the difference between the LL and the PL is known as the plasticity index (PI)
plasticity index (PI)
plastic limit
liquid limit
: plasticity index
Liquidity Index (LI)
PL and LL can be determined only on remolded soils
These limits may not apply to the undisturbed soil
The structure of the soil particles in the undisturbed state may be different from that in the disturbed state
The liquidity index is used to reflect the properties of the natural soil
:natural moisture content of the soil
LI: liquidity index

## Slide 14
Permeability
The property that describes how water flows through the soil
the coefficient of permeability (K), is the constant of proportionality of the relationship between the flow velocity and the hydraulic gradient between two points in the soil
: velocity of water in the soil
hydraulic gradient (head loss per unit length )
: coefficient of permeability

## Slide 15
CLASSIFICATION OF SOILS FOR HIGHWAY USE
Soil classification is a method by which soils are systematically categorized according to their probable engineering characteristics
The classification of a given soil is determined by conducting relatively simple tests on disturbed samples of the soil
However, the engineering properties of a given soil can be predicted reliably from its classification, this should not be regarded as a substitute for the detailed investigation of the soil properties
The most commonly used classification systems
AASHTO Classification System
Unified Soil Classification System (USCS)

## Slide 16
AASHTO Classification System
This system has been described by AASHTO as a means for determining the relative quality of soils for use in:
Embankments
Subgrades
Subbases
Bases
The classification is based on its particle size distribution and the Atterberg limits, (LL, and PI).
soils are classified into seven groups, A-1 through A-7, with several subgroups

## Slide 17
Soils are evaluated within each group by using an empirical formula to determine the group index (GI) of the soils, given as
The GI is determined to the nearest whole number

## Slide 18
A-3 soils are clean but poorly graded sands.
Granular soils fall into classes A-1 to A-3 are:
A-2 soils contain significant amounts of silts and clays
A-1 soils consist of well-graded granular materials
A soil with a GI of zero (an indication of a good subgrade material) will be better as a subgrade material than one with a GI of 20 (an indication of a poor subgrade material).
When soils are properly drained and compacted, their value as subgrade material decreases as the GI increases