## Slide 1: Highway Materials Lecture - 12
Designed and presented
By
Asst. Prof. Dr. Raquim Nihad Zehawi

## Slide 2
BITUMINOUS MATERIALS
There are different types of paving binders
Binder: is the material that is used to bind other components of the mix
The binder in flexible pavement is usually the bitumen
The binder in rigid pavement is usually the Portland cement
The binder in stabilized layers under pavement can be lime, cement or any other type
Bitumen refers to the viscous liquid, soled or semi solid material consisting essentially of hydrocarbons and their derivatives, soluble in CS2 and CCL4, substantially non volatile, soften when heated, have strong adhesive properties with colors ranging from dark brown to black.
*Note: some consider that asphalt is the bituminous mixture with aggregate ( bituminous concrete), while other consider asphalt as the American term of bitumen.
**Note: bitumen should be distinguished from tar, that is bitumen is either naturally found or produced by the fractional distillation of crude oil, while tar is produced by the fractional distillation of coal.

## Slide 3
BITUMEN SOURCES
1- Natural Deposits
Natural deposits of asphalt occur as either native asphalt or rock asphalt.
The largest deposit of native asphalt is known to have existed in Iraq several thousand years ago. It was used in ship building industry in Sumeria about 6000 BC.
The properties of native asphalt vary from one deposit to another, particularly with respect to the amount of insoluble material
Rock asphalt is a natural deposit of sandstone or limestone rocks filled with asphalt
2- Petroleum Asphalt
asphalt emulsions
The asphalt materials obtained from the distillation of petroleum are in the form of different types of asphalts, which include asphalt cements
slow-curing liquid asphalts
medium-curing liquid asphalts
rapid-curing liquid asphalts

## Slide 4
Refining Processes
The refining processes used to obtain petroleum asphalts can be divided into two main groups: and
fractional distillation
destructive distillation (cracking)
The fractional distillation process removes the different volatile materials in the crude oil at successively higher temperatures until the petroleum asphalt is obtained as residue. Steam or a vacuum is used to gradually increase the temperature.
Steam distillation is a continuous flow process in which the crude petroleum is pumped through tube stills or stored in batches, and the temperature is increased gradually to facilitate the evaporation of different materials at different temperatures
Destructive Distillation. Cracking processes are used when larger amounts of the light fractions of materials (such as motor fuels) are required.
Intense heat and high pressures are applied to produce chemical changes in the material. temperatures as high as 1100F and pressure higher than 735 lb/in2
The asphalt obtained from cracking is not used widely in paving, because it is more susceptible to weather changes than that produced from fractional distillation.

## Slide 5
DESCRIPTION AND USES OF BITUMINOUS BINDERS
Asphalt Cements
They are semisolid hydrocarbons with certain physiochemical characteristics that make them good cementing agents.
They are also very viscous, and when used as a binder for aggregates in pavement construction, it is necessary to heat both the aggregates and the asphalt cement prior to mixing the two materials
the particular grade of asphalt cement is designated by its penetration and viscosity as an indication of the consistency at a given temperature,
Asphalt cements are used mainly in the manufacture of hot-mix, hot-laid asphalt concrete
The softest grade used for highway pavement construction has a penetration value of 200 to 300, and the hardest has a penetration value of 60 to 70.

## Slide 6
Asphalt Cutbacks
used mainly in cold-laid plant mixes, road mixes (mixed-in-place), and as surface treatments
Slow-Curing Asphalts
can be obtained directly as slow-curing straight run asphalts through the distillation of crude petroleum Or:
as slow-curing cutback asphalts by “cutting back” asphalt cement with a heavy distillate such as diesel oil
They have lower viscosities than asphalt cement and are very slow to harden
Slow-curing asphalts are designated as SC-70, SC-250, SC-800, or SC-3000, where the numbers relate to the approximate kinematic viscosity in centistokes at 60C (140F).
Medium-Curing Cutback Asphalts
Medium-curing (MC) asphalts are produced by fluxing, or cutting back residual asphalt (usually 120 to 150 penetration) with light fuel oil or kerosene
The term medium refers to the medium volatility of the kerosene-type diluter used. Medium-curing cutback asphalts harden faster than slow-curing liquid asphalts
The fluidity of medium-curing asphalts depends on the amount of solvent in the material
These medium-curing asphalts can be used for the construction of pavement bases, surfaces, and surface treatments

## Slide 7
Rapid-Curing Cutback Asphalts
(RC) cutback asphalts are produced by blending asphalt cement with a petroleum distillate that will evaporate easily
Gasoline or naphtha generally is used as the solvent
(RC) is used for jobs similar to those for which the MC series is used
The grade of rapid-curing asphalt required dictates the amount of solvent to be added to the residual asphalt cement.
RC-3000 requires about 15 percent of distillate
RC-70 requires about 40 percent.

## Slide 8
Emulsified Asphalts
produced by breaking asphalt cement, usually of 100 to 250 penetration range, into minute particles and dispersing them in water with an emulsifier.
The minute particles remain in suspension in the liquid phase as long as the water does not evaporate or the emulsifier does not break.
Asphalt emulsions therefore consist of asphalt (55 to 70 percent by weight), water, and an emulsifying agent, which in some cases also may contain a stabilizer.
anionic and cationic asphalts generally are used in highway maintenance and construction
Asphalt emulsions generally are classified as anionic, cationic, or nonionic
The anionic, cationic types have electrical charges surrounding the particles, whereas the nonionic type is neutral
Anionic
Emulsions containing negatively charged particles of asphalt
Cationic
Emulsions having positively charged particles of asphalt

## Slide 9
Blown Asphalts
It is obtained by blowing air through the semisolid residue obtained during the latter stages of the distillation process
The process involves stopping the regular distillation while the residue is in the liquid form
The material is maintained at a high temperature while air is blown through it
Blown asphalts are relatively stiff compared to other types of asphalts and can maintain a firm consistency at the maximum temperature when exposed to the environment.
Blown asphalt generally is not used as a paving material. However, it is very useful as a roofing material, for automobile undercoating, and as a joint filler for concrete pavements
Road Tars
Tars are obtained from the destructive distillation of such organic materials as coal
Tar properties are significantly different from petroleum asphalts
In general, tars are more susceptible to weather conditions than similar grades of asphalts, and they set more quickly when exposed to the atmosphere

## Slide 10
PROPERTIES OF ASPHALT MATERIALS
Resistance to water action
Consistency
Aging and temperature sustainability
Rate of curing
The consistency usually considered under two conditions:
(1) variation of consistency with temperature and
(2) consistency at a specified temperature.

## Slide 11
Variation of Consistency with Temperature
The consistency of any asphalt material changes as the temperature varies
The change in consistency of different asphalt materials may differ considerably even for the same amount of temperature change
If blown semisolid asphalt and a sample of semisolid regular paving-grade asphalt with the same consistency at a given temperature
But at the high temperatures the regular paving-grade asphalt is much softer than the blown asphalt
This property of asphalt materials is known as temperature susceptibility
Consistency at a Specified Temperature
It is essential that when the consistency of an asphalt material is given, the associated temperature also should be given.

## Slide 12
Aging and Temperature Sustainability
Weathering : is the natural deterioration gradually takes place to asphalt materials caused by chemical and physical reaction as a result of the exposure of the asphalt materials to environmental elements, due to which the materials lose their plasticity and become brittle.
weathering must be minimized to make asphalt act successfully for paving.
Durability: the ability of an asphalt material to resist weathering
factors that influence weathering
oxidation
volatilization
temperature
exposed surface area

## Slide 13
Is the chemical reaction that takes place when the asphalt material is attacked by oxygen in the air causes gradual hardening (loss of the plasticity)
oxidation
Is the evaporation of the lighter hydrocarbons from the asphalt material. causes the loss of the plastic characteristics of the asphalt material.
volatilization
temperature
temperature has a significant effect on the rate of oxidation and volatilization
The relationship between temperature increase and increases in rates of oxidation and volatilization is not linear. The rate of organic and physical reactions in the asphalt material approximately doubles for each 10C (50F) increase in temperature.

## Slide 14
exposed surface area
The exposed surface of the material also influences its rate of oxidation and volatilization
direct relationship between surface area and rate of oxygen absorption and loss due to evaporation in grams/cm3/minute
inverse relationship exists between volume and rate of oxidation and volatilization.
the rate of hardening is directly proportional to the ratio of the surface area to the volume.
This fact is taken into consideration when asphalt concrete mixes are designed for pavement construction in that the air voids are kept to the practicable minimum required for stability to reduce the area exposed to oxidation.

## Slide 15
Rate of curing
Curing is defined as the process through which an asphalt material increases its consistency as it loses solvent by evaporation.
Rate of Curing of Cutbacks
the rate of curing of any cutback asphalt material depends on the distillate used
the rate of curing indicates the time that should elapse before a cutback will attain a consistency that is thick enough for the binder to perform satisfactorily.
The rate of curing is affected by both inherent and external factors.
The important inherent factors
Consistency of the base material
Volatility of the solvent
Quantity of solvent in the cutback
The important external factors
Wind velocity across exposed surface
Temperature
Ratio of surface area to volume

## Slide 16
Rate of Curing for Emulsified Asphalts
depend on the rate at which the water evaporates from the mixture.
When weather conditions include high humidity, low temperature, or rainfall immediately following the application of the emulsion, its ability to properly cure is affected adversely.
When weather conditions are favorable, the water is displaced relatively rapidly, and so curing progresses rapidly
A major advantage of cationic emulsions is that they release their water more readily.
The effect of surface and weather conditions on is more critical for anionic emulsions,
Resistance to water action
The asphalt must sustain its ability to adhere to the aggregates even in the presence of water
In hot-mix, hot-laid asphalt concrete, where the aggregates are thoroughly dried before mixing, stripping does not normally occur and so no preventive action is usually taken.
When water is added to a hot-mix, cold-laid asphalt concrete, commercial antistrip additives usually are added to improve the asphalt’s ability to adhere to the aggregates.