## Slide 1
Ex.Lec 4 Extraction of Magnesium from ore oxide
Dr. Ahmed Ameed
Magnesium is the sixth most abundant element in the earth’s crust.
The main sources of magnesium compounds are:
Seawater (magnesium chloride, MgCl2) and minerals:
Dolomite (CaCO3•MgCO3), contain 13%.
Magnesite (MgCO3), contain 29%.
Brucite Mg(OH)2, contain 42%.
There are two principal magnesium extraction processes: silicothermic process and electrolytic process.
  Silicothermic process (Pidgeon process)
The process involves reducing molten magnesium oxide slag by ferrosilicon under low gas pressure at a temperature of about 1400ºC.
The metallic magnesium, formed in the process, evaporates and then condensates away from the hot region.
The condensed magnesium, having purity of 99.95% is then remelt and cast. The Three Steps of the Pidgeon Process
    Calcination of Dolomite, at 1300oC, Highly Endothermic Reaction, CO2 Released both from the reaction, and from Fuel Burned for Process Heat.
CaMg(CO3)2 CaO + MgO + 2CO2
    Ferrosilicon Alloy Production, the Ferrosilicon Alloy Production by Electric Arc through Mixture of Hematite, Quartz Sand, and Coal. Extremely Endothermic Reaction; Emits Toxic CO.

## Slide 2
Ex.Lec 4 Extraction of Magnesium from ore oxide
Dr. Ahmed Ameed
Fe2O3 + 4SiO2 + 11C 2(Fe)Si2 + 11CO
3. Silicothermic Reduction of MgO by Ferrosilicon, at ~1400oC under Vacuum for 8- 10 hrs. Highly Endothermic Reaction, the ratio of feed are 6 calcine dolomite: 1 ferrosilicon as briquettes.
2MgO + 2CaO + (Fe)Si 2Mg(g) + Ca2SiO4(s) + Fe
II. Dow Process (Electrolysis)
The Dow Process is generally applied for extraction of Magnesium from Sea water. In this process first we add lime for thickening then mix with 10% HCl.
The electrolytic cell consists of a brick-lined vessel, divided into anode and cathode compartments by a semi-wall. Air- or water- cooled Graphite plate anode and steel cathode are submerged in electrolyte composed of

## Slide 3
Ex.Lec 4 Extraction of Magnesium from ore oxide Dr. Ahmed Ameed
alkaline chlorides with addition of magnesium chloride. The operating temperature is 680°C to 750°C. Magnesium chloride decomposes in the electrolytic cell according to the reaction:
MgCl2→ Mg + Cl2 (g)
Metallic magnesium is formed at the cathode. It floats up (it is lighter than electrolyte) collecting in the cathode compartment. Chlorine, which is by-product of the process, is collected in the anode compartment.
In this method CaCl2 and NaCl are added to anhydrous MgCl2 to decrease its melting point.
Dow Cell