## Slide 1
Lecture 9 Dr. Suha K. Shihab
METALS FOR CASTING
Most commercial castings are made of alloys rather than pure metals. Alloys are generally easier to cast, and properties of the resulting product are better. Casting alloys can be classified as ferrous or nonferrous. The ferrous category is subdivided into cast iron and cast steel.
Ferrous Casting Alloys
Cast Iron
Cast iron is the most important of all casting alloys. The tonnage of cast iron castings is several times that of all other metals combined.
There are several types of cast iron:
gray cast iron
nodular iron,
(3) white cast iron
(4) malleable cast iron
(5) alloy cast irons
Typical pouring temperatures for cast iron are around 1400ᴼC depending on composition

## Slide 2
Lecture 8 Dr. Suha K. Shihab
2. Steel
The mechanical properties of steel make it an attractive engineering material and the capability to create complex geometries makes casting an appealing process. However, great difficulties are faced by the foundry specializing in steel which are:
the melting point of steel is considerably higher than for most other metals that are commonly cast.
The solidification range for low carbon steels begins at just under 1540ᴼC. This means that the pouring temperature required for steel is very high about 1650ᴼC .
At these high temperatures, steel is chemically very reactive.
It readily oxidizes, so special procedures must be used during melting and pouring to isolate the molten metal from air.
molten steel has relatively poor fluidity, and this limits the design of thin sections in components cast out of steel.
characteristics of steel castings make it worth the effort to solve these problems.
Tensile strength is higher than for most other casting metals, ranging upward from about 410 MPa.
Steel castings have better toughness than most other casting alloys.

## Slide 3
Lecture 9 Dr. Suha K. Shihab
The properties of steel castings are isotropic; strength is virtually the same in all directions. By contrast, mechanically formed parts (e.g., rolling, forging) exhibit directionality in their properties. Depending on the requirements of the product, isotropic behavior of the material may be desirable.
steel castings is ease of welding. They can be readily welded without significant loss of strength, to repair the casting, or to fabricate structures with other steel components.
Nonferrous Casting Alloys
Nonferrous casting metals include alloys of aluminum, magnesium, copper, tin, zinc, nickel, and titanium.
Aluminum alloys :
Properties that make them attractive include:
generally considered to be very castable.
The melting point of pure aluminum is 660C so pouring temperatures for aluminum casting alloys are low compared to cast iron and steel.
Their properties make them attractive for castings: light weight, wide range of strength properties attainable through heat treatment, and ease of machining.
2. Magnesium alloys :
the lightest of all casting metals.
High corrosion resistance,
high strength-to-weight and stiffness-to-weight ratios.

## Slide 4
Lecture 9 Dr. Suha K. Shihab
Copper alloys: include bronze, brass, and aluminum bronze.
Properties that make them attractive include:
corrosion resistance
attractive appearance
good bearing qualities.
limitation on the use of its alloys is
the high cost of copper
Applications include: pipe fittings, marine propeller blades, pump components, and ornamental jewelry.
Tin-based alloys
Properties that make them attractive include:
generally easy to cast.
Tin has the lowest melting point of the casting metals.
They have good corrosion resistant
limitation on the use of its alloys are
poor mechanical strength, which limits their applications to pewter mugs and similar products not requiring high strength.

## Slide 5
Lecture 9 Dr. Suha K. Shihab
Zinc alloys commonly used in die casting.
Properties that make them attractive include
Zinc has a low melting point
good fluidity, making it highly castable.
limitation on the use of its alloys is
low creep strength, so its castings cannot be subjected to prolonged high stresses.
Nickel alloys
Properties that make them attractive include:
have good hot strength and corrosion resistance, which make them suited to high-temperature applications such as jet engine and rocket components, heat shields, and similar components.
limitation make it and its alloys difficult to cast.
Nickel alloys also have a high melting point and are not easy to cast.
Titanium alloys
Properties that make them attractive include:
for casting are corrosion resistant and possess high strength to-weight ratios.
limitation make it and its alloys difficult to cast.
titanium has a high melting point
low fluidity,
a propensity to oxidize at high temperatures. These properties make it and its alloys difficult to cast.