## Slide 1
Pure Metals : Nucleation & Growth
Solidification does not happen on cooling instantaneously on cooling below Tm
and takes place via nucleation and growth.
Nucleation:
 homogeneous – rare and only if very large undercooling ∆T;
 heterogeneous – on mould walls and/or “impurities”
(including deliberate alloy additions to grain refine microstructure)
Growth may be affected by temperature gradients and preferred crystal growth
directions.
Homogeneous Nucleation
When a solid forms within its own liquid without aid of foreign materials
 nucleate homogeneously .
Homogeneous nucleation requires a large driving force (undercooling)
because of the relatively large contribution of surface energy to the total free energy of small particles.
Heterogeneous Nucleation
Nucleation occurs on preferential sites , such that a solid forms in contact
with a impurity particles, i.e. nucleation agent or mold walls 
heterogeneous nucleation.
Many liquid metals start solidification in a few degrees of supercooling.
Solidification of materials
2

## Slide 2
F f li id t t T b l 
Homogeneous Nucleation
(I)
Free energy of liquid at a temp. ΔT below Tm  G1
G1  (VS  VL )GV
If some of atoms of liquid cluster together form a small cluster sphere of solid, the free energy of the system will change to G2
L
S
L
G2  VSGV  VLGV 
ASL  SL
VS : volume of solid sphere,
VL : volume of liquid
G S , G L : free energies per unit volume of solid and liquid respectively
V
V
ASL : solid/liquid interfacial area, SL : solid/liquid interfacial free energy
Free energy change due to the formation of solid
ΔG  G2  G1
 V (GL  GS )  A 
S V
V
SL SL
 VS ΔGV 
ASL  SL
ΔGv is positive below Tm , so that
 Negative contribution due to the lower free energy of a bulk solid
 Positive contribution due to the creation of solid/liquid interface
Solidification of materials
3

## Slide 3
Homogeneous Nucleation (II)
ΔG  VS ΔGV 
ASL  SL
The excess free energy associated with the solid particles can be minimized by
the formation of sphere of radius r
ΔG   4 r3 ΔG
3
 4r2

V
SL
If a very small solid particle forms, the retarding energy (ΔGs) term is larger
than the driving energy (ΔGv).
 the creation of small solid particles leads to a free energy increase.
 liquid phase is able to maintain in a metastable state almost infinitely at
temperatures below Tm.
Solidification of materials
4

## Slide 4
i ll d i i l di f l i l hi h bl h
Homogeneous Nucleation
(III)
ΔG   4 r3 ΔG
3
 4r2

V
SL
At a given ΔT,
If r < r*, a small increase in radius Δr results
in an
increase
of the total
free energy which is not a spontaneous process.
 the system can lower its free energy by dissolution of solid particle
 unstable solid particles with r < r*,  embryos
Only if r > r*, the growth of solid proceeds spontaneously with decrease
in free energy of the system.
 the system can decrease its free energy by growth of solid particle
 stable solid particles with r > r*,  nuclei
r* is called as critical radius of "nuclei" (clusters which are able the grow).
At the critical radius the total free energy change has a maximum ΔG* which
is known as nucleation barrier.
Solidification of materials
5

## Slide 5
di li id
G
Homogeneous Nucleation (IV)
Estimation of the size of the critical radius
dG = 0 when r = r*  the critical nucleus is in equilibrium with the surrounding liquid
Differentiation of the total free energy equation with
respect
to
r,
and
 0 ,
at r = r*
r r*
ΔG   4 r3 ΔG
3
 4r2 
V
SL
dΔG
dr
 4r*2 ΔG  8r* 
 0
V
SL
r r *
and therefore,
r 2 SL
⎛ 2 SL Tm
⎞ 1


⎜
⎝
⎟
ΔGV
L ⎠ ΔT
3
3 2
⎛ 16 T
⎞
16
1
SL ⎜ SL m ⎟ 
ΔG 

⎜
3L2 ⎟ (ΔT)2
)2
3(ΔG
⎝
⎠
V
The size of r* is reduced by greater undercooling (ΔT), this means that
smaller nuclei are able to grow.
Without undercooling, the nucleation will not start (if ΔT = 0, then r* 
∞).
The nucleation barrier ΔG* is also inversely related to ΔT: the nucleation
barrier decreases as the undercooling increases.
Solidification of materials
6
dΔG
dr

## Slide 6
Homogeneous
Nucleation
(V)
For
FCC
Copper, r*1 nm,
which
contains
310
Cu
atoms
in
each
nucleus.
A solid sphere of r will have a free energy greater than that of bulk
solid by 2r per unit volume.
Solidification of materials
7

## Slide 7
Homogeneous Nucleation (VI)
Formation of solid nucleus
Many small close-packed clusters of atoms (crystalline atomic array)
present in the liquid
Total number of atoms in liquid, n0
The number of spherical clusters of radius r, nr
ΔGr )
n  n exp(
r
0
kT
ΔGr : the excess free energy associated with cluster,
k : Boltzmann constant
For a liquid above Tm , this relationship applied for all values of r,
but for a solid, the relationship only applied for r ≤ r*
Since nr decreases exponentially with ΔGr (which itself increases rapidly
with r), the probability of finding a given cluster decreases very rapidly as
the cluster size increases
for example) at Tm, Cu (1020 atoms/mm3) contains ~1015 clusters of
0.3 nm (~10 atoms) and ~10 clusters of 0.6 nm (~100 atoms)
Maximum size of clusters in the liquid
increases with decreasing temperature.
Critical nucleus size r*  1/ΔT
For supercollings of DTN or greater,
 some clusters reaches r*, and growing into stable solid particles
Solidification of materials
8

## Slide 8
( /kT) th d i b i t j i t t iti l l
6
⎢
Homogeneous Nucleation (VII)
Homogeneous Nucleation Rate
The cluster with a critical radius r* will convert stable nucleus by addition of
a single atom to a critical nucleus
P : frequency with which the addition of a single atom to a critical nucleus makes that nucleus is supercritical and able to grow rapidly
1n
ΔGi )
kT
P 
 exp(
L
6
1/6 : possibility with which atom directs to the L/S interface
nL


: the number of atoms surrounding a critical nucleus
: atomic vibration frequency (~kT / h, h : Plank constant)
: possibility with which each atom jumps across the L/S interface
exp (-ΔGi/kT) : thermodynamic barrier to join atom to critical nucleus
- Nucleation Rate,
Nhom

1n
6
ΔGr ΔGi )
N  n P 
n  exp(
hom
r
0 L
kT

n0kT
h
n0kT
ΔGr )

exp(
kT
A ⎤
2 ⎥
3 2
16SL Tm
⎡
exp
A 

⎢
2
3L kT
h
(ΔT)
⎣
⎦
At low undercoolings,
the nucleation barrier is
high and the rate of nucleus formation is low.
Greater undercooling promotes the nucleation
due to decrease in r* and ΔG*.
Solidification of materials
9