## Slide 1: Lecture Eleven Casting Quality
There are numerous opportunities for things to go wrong in a casting operation, resulting in quality defects in the product
The defects can be classified as follows:
  General defects common to all casting processes
  Defects related to sand casting process

## Slide 2
A casting that has solidified before completely filling mold cavity
General Defects:
Misrun

## Slide 3
Two portions of metal flow together but there is a lack of fusion due to premature freezing
General Defects:
Cold Shut

## Slide 4
Metal splatters during pouring and solid globules form and become entrapped in casting
General Defects:
Cold Shot

## Slide 5
Depression in surface or internal void caused by solidification shrinkage that restricts amount of molten metal available in last region to freeze
General Defects:
Shrinkage Cavity

## Slide 6
Balloon‑shaped gas cavity caused by release of mold gases during pouring
Sand Casting Defects:
Sand Blow

## Slide 7
Formation of many small gas cavities at or slightly below surface of casting
Sand Casting Defects:
Pin Holes

## Slide 8
When fluidity of liquid metal is high, it may penetrate into sand mold or core, causing casting surface to consist of a mixture of sand grains and metal
Sand Casting Defects:
Penetration

## Slide 9
A step in the cast product at parting line caused by sidewise relative displacement of cope and drag
Sand Casting Defects:
Mold Shift

## Slide 10: Foundry Inspection Methods
Visual inspection to detect obvious defects such as misruns, cold shuts, and severe surface flaws
Dimensional measurements to insure that tolerances have been met
Metallurgical, chemical, physical, and other tests concerned with quality of cast metal