## Slide 1: Lecture Three Desirable Mold Properties
Strength ‑ to maintain shape and resist erosion
Permeability ‑ to allow hot air and gases to pass through voids in sand
Thermal stability ‑ to resist cracking on contact with molten metal
Collapsibility ‑ ability to give way and allow casting to shrink without cracking the casting
Reusability ‑ can sand from broken mold be reused to make other molds?

## Slide 2: Foundry Sand
Silica (SiO2) or silica mixed with other minerals
  Good refractory properties ‑ for high temperatures
  Small grain size for better surface finish on part
  Large grain size is more permeable, allowing gases to escape during pouring
  Irregular grain shapes strengthen molds due to interlocking, compared to round grains
    Disadvantage: interlocking reduces permeability

## Slide 3: Binders Used with Foundry Sand
Sand is held together by a mixture of water and bonding clay
  Typical mix: 90% sand, 3% water, and 7% clay
Other bonding agents also used in sand molds:
  Organic resins (e g , phenolic resins)
  Inorganic binders (e g , sodium silicate and phosphate)
Additives are sometimes combined with the mixture to increase strength and/or permeability

## Slide 4: Types of Sand Mold
Green‑sand molds - mixture of sand, clay, and water
  “Green" means mold contains moisture at time of pouring
Dry‑sand mold - organic binders rather than clay
  Mold is baked to improve strength
Skin‑dried mold - drying mold cavity surface of a green‑sand mold to a depth of 10 to 25 mm, using torches or heating lamps

## Slide 5: Buoyancy in a Sand Casting Operation
During pouring, buoyancy of the molten metal tends to displace the core, which can cause casting to be defective
Force tending to lift core = weight of displaced liquid less the weight of core itself
    Fb = Wm ‑ Wc
where Fb = buoyancy force; Wm = weight of molten metal displaced; and Wc = weight of core