## Slide 1: Lecture Seven Investment Casting: Advantages and Disadvantages
Advantages:
  Parts of great complexity and intricacy can be cast
  Close dimensional control and good surface finish
  Wax can usually be recovered for reuse
  This is a net shape process - additional machining is not normally required
Disadvantages:
  Many processing steps are required
  Relatively expensive process

## Slide 2: Plaster Mold Casting
Similar to sand casting except mold is made of plaster of Paris (gypsum ‑ CaSO4‑2H2O)
  In mold-making, plaster and water mixture is poured over plastic or metal pattern and allowed to set
    Wood patterns not generally used due to extended contact with water
  Plaster mixture readily flows around pattern, capturing its fine details and good surface finish

## Slide 3: Plaster Mold Casting: Advantages and Disadvantages
Advantages:
  Good accuracy and surface finish
  Capability to make thin cross sections
Disadvantages:
  Mold must be baked to remove moisture
    Moisture can cause problems in casting
  Mold strength is lost if over-baked
  Plaster molds cannot stand high temperatures
    Limited to lower melting point alloys

## Slide 4: Ceramic Mold Casting
Similar to plaster mold casting except that mold is made of refractory ceramic material that can withstand higher temperatures than plaster
  Can be used to cast steels, cast irons, and other high‑temperature alloys
  Applications similar to those of plaster mold casting except for the metals cast
  Advantages (good accuracy and finish) also similar

## Slide 5: Permanent Mold Casting Processes
Economic disadvantage of expendable mold casting:
  A new mold is required for every casting
In permanent mold casting, the mold is reused many times
Processes include:
  Basic permanent mold casting
  Die casting
  Centrifugal casting

## Slide 6: The Basic Permanent Mold Process
Uses a metal mold constructed of two sections designed for easy, precise opening and closing
  Molds used for casting lower melting point alloys are commonly made of steel or cast iron
  Molds used for casting steel must be made of refractory material, due to the very high pouring temperatures

## Slide 7: Steps in Permanent Mold Casting
(1) Mold is preheated and coated for lubrication and heat dissipation

## Slide 8: Steps in Permanent Mold Casting
(2) Cores (if any are used) are inserted and mold is closed

## Slide 9: Steps in Permanent Mold Casting
(3) Molten metal is poured into the mold, where it solidifies

## Slide 10: Steps in Permanent Mold Casting
(4) Mold is opened

## Slide 11: Permanent Mold Casting: Advantages and Limitations
Advantages of permanent mold casting:
  Good dimensional control and surface finish
  Rapid solidification caused by metal mold results in a finer grain structure, so castings are stronger
Limitations:
  Generally limited to metals of lower melting point
  Simpler part geometries compared to sand casting because of need to open the mold
  High cost of mold

## Slide 12: Applications and Metals for Permanent Mold Casting
Due to high mold cost, process is best suited to high volume production and can be automated accordingly
Typical parts: automotive pistons, pump bodies, and certain castings for aircraft and missiles
Metals commonly cast: aluminum, magnesium, copper‑base alloys, and cast iron
  Unsuited to steels because of very high pouring temperatures