## Slide 1: Lecture Eight Die Casting
A permanent mold casting process in which molten metal is injected into mold cavity under high pressure
  Pressure is maintained during solidification, then mold is opened and part is removed
  Molds in this casting operation are called dies; hence the name die casting
  Use of high pressure to force metal into die cavity is what distinguishes this from other permanent mold processes

## Slide 2: Die Casting Machines
Designed to hold and accurately close two mold halves and keep them closed while liquid metal is forced into cavity
Two main types:
  Hot‑chamber machine
  Cold‑chamber machine

## Slide 3: Hot-Chamber Die Casting
Metal is melted in a container, and a piston injects liquid metal under high pressure into the die
  High production rates
    500 parts per hour not uncommon
  Applications limited to low melting‑point metals that do not chemically attack plunger and other mechanical components
  Casting metals: zinc, tin, lead, and magnesium

## Slide 4: Hot-Chamber Die Casting
Hot‑chamber die casting cycle: (1) with die closed and plunger withdrawn, molten metal flows into the chamber

## Slide 5: Hot-Chamber Die Casting
(2) plunger forces metal in chamber to flow into die, maintaining pressure during cooling and solidification.

## Slide 6: Hot-Chamber Die Casting
(3) Plunger is withdrawn, die is opened, and casting is ejected

## Slide 7: Cold‑Chamber Die Casting Machine
Molten metal is poured into unheated chamber from external melting container, and a piston injects metal under high pressure into die cavity
  High production but not usually as fast as hot‑chamber machines because of pouring step
  Casting metals: aluminum, brass, and magnesium alloys
  Advantages of hot‑chamber process favor its use on low melting‑point alloys (zinc, tin, lead)

## Slide 8: Cold‑Chamber Die Casting Cycle
(1) With die closed and ram withdrawn, molten metal is poured into the chamber

## Slide 9: Cold‑Chamber Die Casting Cycle
(2) Ram forces metal to flow into die, maintaining pressure during cooling and solidification

## Slide 10: Cold‑Chamber Die Casting Cycle
(3) Ram is withdrawn, die is opened, and part is ejected

## Slide 11: Molds for Die Casting
Usually made of tool steel, mold steel, or maraging steel
Tungsten and molybdenum (good refractory qualities) used to die cast steel and cast iron
Ejector pins required to remove part from die when it opens
Lubricants must be sprayed onto cavity surfaces to prevent sticking

## Slide 12
A die casting that measures about 400 mm diagonally for a truck cab floor (courtesy of
George E. Kane Manufacturing Technology Laboratory)

## Slide 13: Die Casting: Advantages and Limitations
Advantages:
  Economical for large production quantities
  Good accuracy and surface finish
  Thin sections possible
  Rapid cooling means small grain size and good strength in casting
Disadvantages:
  Generally limited to metals with low metal points
  Part geometry must allow removal from die