## Slide 1: FORTH YEAR – CERAMIC
REVIEWING QUESTIONS
Q1/ For refractory ceramic materials, cite three characteristics that improve with and two characteristics that are adversely (negatively) affected by increasing porosity.
Answer/
The noticeable properties of these materials include the
capacity to withstand high temperatures without melting or decomposing, and the capacity to remain unreactive or inert when exposed to severe (difficult) environments. In addition, the ability to provide thermal insulation is often an important consideration.
Refractory materials are marketed in a variety of forms, but bricks are the most common. Typical applications include furnace coatings for metal purifying, glass

## Slide 2: FORTH YEAR – CERAMIC
manufacturing, metallurgical heat treatment, and power
generation.
Porosity is one microstructural variable (changeable) that must be controlled to produce a suitable refractory brick. Strength, load-bearing capacity, and resistance to attack by corrosive materials all increase with porosity reduction. At the same time, thermal insulation characteristics and resistance to thermal shock are diminished (reduced). Of course, the optimum porosity depends on the conditions of service.
Q2/ Compare the manner in which the aggregate particles become bonded together in clay-based mixtures during firing and in cements during setting.
Answer/
Several familiar ceramic materials are classified as inorganic cements: cement, plaster of Paris, and lime,

## Slide 3: FORTH YEAR – CERAMIC
which, as a group, are produced in extremely large
quantities. The characteristic feature of these materials is that when mixed with water, they form a paste that subsequently sets and hardens. This feature is especially useful in that solid and rigid structures having just about any shape may be formed. Also, some of these materials act as a bonding phase that chemically binds particulate aggregates into a single cohesive (interconnected) structure. Under these circumstances, the role of the cement is similar to that of the glassy bonding phase that forms when clay products and some refractory bricks are fired. One important difference, however, is that the bond between the cement particles develops at room temperature.
Q4/ what is meant b lime, gypsum and plaster Answer/

## Slide 4: FORTH YEAR – CERAMIC
They are types of cement materials. First, plaster is a
white powder (a form of calcium sulphate) that forms a paste when mixed with water and hardens into a solid, use in making molds and cast for broken limbs (/b silent/ (arms, legs.)
While lime, is a calcium oxide, white alkaline substance obtained by heating calcium carbonate at high temperature, used usually in building.
Finally, Gypsum (CaSO4–2H2O) (hydrate calcium sulphate) is colorless or white mineral form used to make cements and plasters especially plaster of Paris.
Q3/ To which group the Portland cement is classified, define it and explain the method of its production.
Answer/
Portland cement is a type of cement materials. This product is consumed in the largest weights. It is produced

## Slide 5: FORTH YEAR – CERAMIC
by grinding and well mixing clay and lime-bearing minerals in the proper proportions, and then heating the mixture to about 1400 0C in a rotary kiln (furnace); this process,
sometimes called chemical changes
calcination, produces physical and in the raw materials. The resulting
“clinker” product is then ground into a very fine powder to which is added a small amount of gypsum (CaSO4–2H2O) (hydrate calcium sulphate) to retard (delay/ hold back) the setting process. The properties of Portland cement, including setting time and final strength, to a large degree depend on its composition. Several different constituents are found in Portland cement, the principal ones being tricalcium silicate (3CaO–SiO2) and dicalcium silicate (2CaO–SiO2). The setting and hardening of this material result from relatively complicated hydration reactions that occur among the various cement constituents and the water that is added. For example, one hydration reaction involving dicalcium silicate is as follows:
2CaO–SiO2 + xH2O = 2CaO–SiO2–xH2O

## Slide 6: FORTH YEAR – CERAMIC
where x is variable and depends on how much water is available. These hydrated products are in the form of complex gels or crystalline substances that form the cementitious bond. Hydration reactions begin just as soon as water is added to the cement. These are first revealed as setting (i.e., the stiffening of the once-plastic paste), which takes place soon after mixing, usually within several hours. Hardening of the mass follows as a result of further hydration, a relatively slow process that may continue for as long as several years. It should be emphasized that the process by which cement hardens is not one of drying but, rather, of hydration in which water actually participates in a chemical bonding reaction. Portland cement is termed a hydraulic cement because its hardness develops by chemical reactions with water. It is used primarily in mortar and concrete to bind, into a cohesive mass, aggregates of inert particles (sand and/or gravel); these are considered to be composite materials. Other cement materials, such as lime, are nonhydraulic; that is, compounds other than water (e.g., CO2) are involved in the hardening reaction.

## Slide 7
FORTH YEAR – CERAMIC