## Slide 1
Chapter 5 AUXILIARY FUNCTIONS*
5.1 INTRODUCTION
The main power of the thermodynamic method stems from its provision of criteria for equilibrium in materials systems and its determination of the influence, on an equilibrium state, of changes in the external influences acting on the system. The practical usefulness of this power is, however, determined by the practicality of the equations of state for the system, i.e., the relationships which can be established among the thermodynamic properties of the system.
Combination of the First and Second Laws of Thermodynamics leads to the derivation of Eq. (3.12)
This equation of state gives the relationship between the dependent variable U and the independent variables S and V for a closed system of fixed composition which is undergoing a process involving a change of volume against the external pressure as the only form of work performed on, or by, the system. Combination of the First and Second Law also provides the criteria for equilibrium that
In a system of constant internal energy and constant volume, the entropy has its maximum value, and
In a system of constant entropy and constant volume, the internal energy has its minimum value.
The further development of thermodynamics beyond Eq. (3.12) arises, in part, from the fact that, from a practical point of view, S and V are an inconvenient choice of independent variables. Although the volume of a system can be measured with relative ease and, in principle, can be controlled, entropy can be neither simply measured nor simply controlled. It is thus desirable to develop a simple expression, similar in form to Eq. (3.12), which contains a more convenient choice of independent variables and which can accommodate changes in the composition of the system. From a practical point of view the most convenient pair of independent variables would be temperature and pressure, as these variables are most easily measured and controlled. The derivation of an equation of state of the simple form of Eq. (3.12), but using P and T as the independent variables, and a criterion for equilibrium in a constant-pressure constant-temperature system are thus desirable. Alternatively, from the theoretician’s point of view the most convenient choice of independent variables would be V and T, as constant-volume
*The derivation of the auxiliary functions is presented in Appendix C.

## Slide 2
98 Introduction to the Thermodynamics of Materials
constant-temperature systems are most easily examined by the methods of statistical mechanics. This arises because fixing the volume of a closed system fixes the quantization of its energy levels, and thus the Boltzmann factor, exp(–si/kT), and the
partition function, both of which appear in Eq. (4.13), have constant values in constant- volume constant-temperature systems. The derivation of an equation of state using T and V as the independent variables and the establishment of a criterion for equilibrium in a system of fixed volume and fixed temperature are thus desirable.
Eq. (3.12) cannot be applied to systems which undergo changes in composition caused by chemical reactions or to systems which perform work other than work of expansion against an external pressure (so-called P-V work). As systems which experience changes in composition, such as the transfer of an impurity element from a metal to a refining slag or the precipitation of a second phase in a ceramic oxide, are of prime importance to the materials engineer, composition variables must be included in any equation of state and in any criterion for equilibrium. Also any equation of state must be capable of accommodating forms of work other than P-V work, such as the electrical work performed by a galvanic cell.
Thus, although Eq. (3.12) lays the foundation of thermodynamics, it is necessary to develop auxiliary thermodynamic functions, which, as dependent variables, are related in simple form to more convenient choices of independent variables. Also, with this increase in the number of thermodynamic functions, it is necessary to establish the relationships which exist among them. It is often found that some required thermodynamics expression which, itself, is not amenable to experimental measurement is related in a simple manner to some measurable quantity. Examples of this have been presented in Chap. 3, where it was found that (6U/6S)V=T, –(6U/6V)S=P, and
(6S/6V)U=P/T.
In this chapter the thermodynamic functions A (the Helmholtz free energy), G (the Gibbs free energy), and µi (the chemical potential of the species i) are introduced, and
their properties and interrelationships are examined. The functions A and G are defined as
(5.1)
and
(5.2)
5.2 THE ENTHALPY H
As has been seen in Chap. 2, for a closed system undergoing a change of state at constant pressure, P, from the state 1 to the state 2, the First Law gives

## Slide 3
Auxiliary Functions 99
which, on rearrangement, gives
or
Thus, when a closed system undergoes a change of state at constant pressure (during which only P-V work is done), the change in the enthalpy of the system equals the heat entering or leaving the system. The properties of H are examined in detail in Chap. 6.
5.3 THE HELMHOLTZ FREE ENERGY A
For a system undergoing a change of state from state 1 to state 2, Eq. (5.1) gives
and, if the system is closed,
in which case
If the process is isothermal, that is, T2=T1=T, the temperature of the heat reservoir which supplies or withdraws heat during the process, then, from the Second Law, Eq. (3.4a),
and hence
Comparison with Eq. (3.11) shows that the equality can be written as

## Slide 4
100 Introduction to the Thermodynamics of Materials
(5.3)
and thus, during a reversible isothermal process, for which OSirr is zero, the amount of work done by the system wmax is equal to the decrease in the value of the Helmholtz free
energy. Furthermore, for an isothermal process conducted at constant volume, which, necessarily, does not perform P-V work, Eq. (5.3) gives
(5.4)
or, for an increment of such a process,
As dSirr is always positive during a spontaneous process it is thus seen that A decreases during a spontaneous process, and as dSirr=0 is a criterion for a reversible process, equilibrium requires that
(5.5)
Thus in a closed system held at constant T and V, the Helmholtz free energy can only decrease or remain constant, and equilibrium is attained in such a system when A achieves its minimum value. The Helmholtz free energy thus provides a criterion for equilibrium in a system at constant temperature and constant volume.
This criterion can be illustrated by examination of the following system. Consider n atoms of some element occurring in both a solid crystalline phase and a vapor phase contained in a constant-volume vessel, which, in turn, is immersed in a constant- temperature heat reservoir. The problem involves determining the equilibrium distribution of the n atoms between the solid phase and the vapor phase. At constant volume and constant temperature this distribution must be that which gives the Helmholtz free energy its minimum value. From Eq. (5.1)
which shows that low values of A are obtained with low values of U and high values of S. The two extreme states of existence which are available to the system are
1. That in which all of the atoms exist in the solid crystalline phase and none occurs in the vapor phase, and

## Slide 5
Auxiliary Functions 101
2. That in which all of the atoms exist in the vapor phase and none occurs in the solid phase.
Consider the system occurring in the first of these two states. The equilibrium distance between the centers of neighboring atoms in a solid phase is that at which there is a balance between the attractive and repulsive forces operating between the atoms, and thus, if an atom is to be removed from the surface of a solid and placed in a gas phase, work must be done against the attractive forces operating between the atom and its neighbors. For the separation of the atom to be conducted isothermally, the energy required for the separation must be supplied as heat which flows from the heat reservoir. This flow of heat into the system increases both the internal energy and the entropy of the constant-volume system. A system comprising 1 atom in the vapor phase and n–1 atoms in the solid phase is more random than the system comprising n atoms in the solid phase, and hence the entropy of the former is greater than that of the latter.
As more atoms are removed from the solid and placed in the vapor phase, heat continues to flow from the heat reservoir, and the internal energy and the entropy of the system continue to increase. Eventually when all n atoms occur in the vapor phase, the internal energy and the entropy of the constant-volume constanttemperature system have their maximum values. In contrast, the state in which all of the n atoms occur in the solid is that in which the internal energy and the entropy have their minimum values. The variations of the internal energy and the entropy of the system with the number of atoms occurring in the vapor phase, nv, are shown, respectively, in Figs. 5.1a and b. As the
transfer of an atom from the solid to the vapor causes a fixed increment in the internal energy of the system, the internal energy increases linearly with nv as shown in Fig. 5.1a.
In contrast, as the magnitude of the increase in the disorder in the system, caused by the transfer of an atom from the solid to the vapor, decreases with increasing number of atoms in the vapor phase, the entropy of the system, shown in Fig. 5.1b, is not a linear function of nv; the rate of increase of S decreases with increasing nv. The variation of A,
which is obtained as the sum of U and –TS, with nv is shown in Fig. 5.2. This figure shows that A has a minimum value at a unique value of nv, designated as nv(eq.T). This

## Slide 6
102 Introduction to the Thermodynamics of Materials
Figure 5.1 The variations of (a) internal energy, U, and (b) entropy, S, with the number of atoms in the vapor phase of a closed solidvapor system at constant temperature and constant volume.
Figure 5.2 Illustration of the criterion for equilibrium in a closed solidvapor system at constant temperature and constant volume.

## Slide 7
Auxiliary Functions 103
state is the compromise between minimization of U and maximization of S, and in this state the solid exerts its equilibrium vapor pressure at the temperature T. If the vapor behaves ideally, then the vapor pressure, which is called the saturated vapor pressure, is given by
in which V is the volume of the containing vessel, Vs is the volume of the solid phase
present, and k is Boltzmann’s constant. The saturated vapor pressure is proportional to the concentration of atoms in the vapor phase, nv(eq,T)/(V–VS), and is thus not dependent on
the volume in the system available to the vapor phase. As the magnitude of the entropy contribution, –TS, increases with increasing temperature and the internal energy contribution is independent of temperature, the contribution of the entropy term to A becomes increasingly predominant as the temperature is increased, and the compromise between U and –TS which minimizes A occurs at larger values of nv (or larger
concentrations of atoms in the vapor phase). This is illustrated in Fig. 5.3 which is drawn for the temperatures T1 and T2, where T1<T2. An increase in the temperature from T1 to
T2 increases the saturated vapor pressure of the solid from
to
In general the saturated vapor pressures of solids and liquids increase exponentially with increasing temperature. For example, the saturated vapor pressure of solid CO2, “dry

## Slide 8
104 Introduction to the Thermodynamics of Materials
Figure 5.3 The influence of temperature on the equilibrium state of a closed solid-vapor system of constant volume.
The saturated vapor pressure of dry ice thus increases from 0.01 atm at 151.2 K, to 0.1 atm at 170.2 K, to 1 atm at 194.6 K.
For the constant-volume system the maximum temperature at which both solid and vapor phases occur is that temperature at which minimization of A occurs at n=nv. Above
this temperature the entropy contribution overwhelms the internal energy contribution, and hence all n atoms occur in the vapor phase. At such temperatures the pressure in the vessel is less than the saturated value, and the solid phase could only be made to reappear by either decreasing the volume of the system or increasing the number of atoms in the system, both of which increase the concentration of atoms in the vapor phase. Conversely, the concentration of atoms in the vapor phase decreases with decreasing temperature, and, in the limit T → 0 K, the entropy contribution to A vanishes and minimization of A coincides with minimization of U. Consequently, all of the n atoms occur in the solid phase.
If the constant-temperature heat reservoir containing the constant-volume system is, itself, of constant volume and is adiabatically contained, then the combined system is one

## Slide 9
Auxiliary Functions 105
of constant U and constant V. Thus the occurrence of the equilibrium concentration of atoms in the vapor phase coincides with the combined system having a maximum entropy. This is illustrated as follows. The entropy of the combined system is equal to the sum of the entropy of the heat reservoir and the entropy of the constant-volume particles system contained within it. The flow of heat from the reservoir to the particles system decreases the entropy of the former and increases the entropy of the latter. However, if less than the equilibrium number of atoms occurs in the vapor phase, then spontaneous evaporation of the solid occurs until the saturated vapor pressure is reached. During this process heat q flows spontaneously from the heat reservoir to the particles system, the entropy of the reservoir decreases by the amount q/T, the entropy of the particles system increases by the amount q/T+OSirr, and the increase in the entropy of the combined
system is OSirr. From Eq. (5.4) the corresponding decrease in the Helmholtz free energy is
and hence minimization of A in the constant T, constant V particles system corresponds to maximization of S in the constant U, constant V combined system.
Classical Thermodynamics is concerned only with equilibrium states, and hence only that single state at the given values of V and T at which A has its minimum value is of interest from the point of view of thermodynamic consideration. In contrast, from the viewpoint of statistical mechanics all values of nv in the range 0≤nv≤n are possible at the
given values of V and T, although the probability than nv deviates from the equilibrium value of nv(eq,T) is exceedingly small. This probability is small enough that, in practical
terms, it corresponds with the thermodynamic statement that spontaneous deviation of a system from its equilibrium state is impossible.
5.4 THE GIBBS FREE ENERGY G
For a system undergoing a change of state from 1 to 2, Eq. (5.2) gives
For a closed system, the First Law gives
and thus

## Slide 10
106 Introduction to the Thermodynamics of Materials
(5.6)
If the process is carried out such that T1=T2=T, the constant temperature of the heat reservoir which supplies or withdraws heat from the system, and also if P1=P2=P, the constant pressure at which the system undergoes a change in volume, then
In the expression for the First Law the work w is the total work done on or by the system during the process. Thus if the system performs chemical or electrical work in addition to the work of expansion against the external pressure, then these work terms are included in w. Thus w can be expressed as
in which P(V2–V1) is the P-V work done by the change in volume at the constant pressure
P and w is the sum of all of the non-P-V forms of work done. Substituting into Eq. (5.6) gives
and again, as
then
(5.7)
Again, the equality can be written as
Thus, for an isothermal, isobaric process, during which no form of work other than P-V
work is performed, i.e., w=0
(5.8)

## Slide 11
Now,
(5.10)
(5.11)
(5.12)
5.6 THE VARIATION OF THE COMPOSITION AND SIZE OF THE SYSTEM
The discussion thus far has been restricted to consideration of closed systems of fixed size and fixed composition, and in such cases it was found that the system has two independent variables which, when fixed, uniquely, fixed the state of the system. However, if the size and composition can vary during a process, then the specification of only two variables is no longer sufficient to fix the state of the system. For example, it has been shown that, for a process conducted at constant temperature and constant pressure, equilibrium is attained when G attains its minimum value. If the composition of
Auxiliary Functions 107
Such a process can only occur spontaneously (with a consequent increase in entropy) if the Gibbs free energy decreases. As dSirr=0 is a criterion for thermodynamic equilibrium, then an increment of an isothermal isobaric process occurring at equilibrium requires that
(5.9)
Thus, for a system undergoing a process at constant T and constant P, the Gibbs free energy can only decrease or remain constant, and the attainment of equilibrium in the system coincides with the system having the minimum value of G consistent with the values of P and T. This criterion of equilibrium, which is of considerable practical use, will be used extensively in the subsequent chapters.
5.5 SUMMARY OF THE EQUATIONS FOR A CLOSED SYSTEM
Eq. (3.12) gives

## Slide 12
108 Introduction to the Thermodynamics of Materials
the system is variable, in that the numbers of moles of the various species present can vary as the consequence of a chemical reaction occurring in the system, then minimization of G at constant P and T occurs when the system has a unique composition. For example, if the system contained the gaseous species CO, CO2, H2, and H2O, then at
constant T and P minimization of G would occur when the reaction equilibrium CO+H2O=CO2+H2 was established. Similarly, as G is an extensive property, i.e., is
dependent on the size of the system, it is necessary that the number of moles within the system be specified.
The Gibbs free energy, G, is thus a function of T, P, and the numbers of moles of all of the species present in the system, i.e.,
(5.13)
in which ni, nj, nk, nk,…are the numbers of moles of the species i, j, k,…present in the
system and the state of the system is only fixed when all of the independent variables are fixed. Differentiation of Eq. (5.13) gives
(5.14)
If the numbers of moles of all of the individual species remain constant during the process, Eq. (5.14) simplifies to Eq. (5.12), i.e.,
from which it is seen that
and

## Slide 13
Auxiliary Functions 109
Substitution into Eq. (5.14) gives
(5.15)
where
is the sum of k terms (one for each of the k species) each of which is determined by partial differentiation of G with respect to the number of moles of the ith species at constant T, P, and nj, where nj represents the numbers of moles of every species other
than the ith species.
5.7 THE CHEMICAL POTENTIAL
The term (6G/6ni)T,p,nj,…. is called the chemical potential of the species i and is designated as µi, i.e.,
(5.16)
The chemical potential of i in a homogeneous phase is thus the rate of increase of G with
ni when the species i is added to the system at constant temperature, pressure, and
numbers of moles of all of the other species. Alternatively, if the system is large enough that the addition of 1 mole of i, at constant temperature and pressure, does not measurably change the composition of the system, then µi is the increase in the Gibbs
free energy of the system caused by the addition.
Eq. (5.15) can thus be written as
(5.17)
in which from G is expressed as a function of T, P, and composition. Eq. (5.17) can thus be applied to open systems which exchange matter as well as heat with their surroundings, and to closed systems which undergo changes in composition caused by chemical reactions.

## Slide 14
110 Introduction to the Thermodynamics of Materials
Similarly, Eqs. (3.12), (5.10), and (5.11) can be made applicable to open systems by including the terms describing the dependences on composition of, respectively, U, H, and A:
(5.18)
(5.19)
(5.20)
Inspection of Eqs. (5.16), (5.18), (5.19), and (5.20) shows that
(5.21)
and, hence, the complete set of equations is
(5.22)
(5.23)
(5.24)
(5.25)
U is thus the “characteristic function” of the independent variables S, V, and composition, H is the characteristic function of the independent variables S, P, and composition, A is the characteristic function of the independent variables T, V, and composition, and G is the characteristic function of the independent variables T, P, and composition. Although all four of the above equations are basic in nature, Eq. (5.25) is called the fundamental equation because of its practical usefulness.

## Slide 15
Auxiliary Functions 111
The First Law gives
which, on comparison with Eq. (5.22), indicates that, for a closed system undergoing a process involving a reversible change in composition (e.g., a reversible chemical reaction),
and
The term Z µidni is thus the chemical work done by the system which was denoted as w
 in Eq. (5.8), and the total work w is the sum of the P-V work and the chemical work.
5.8 THERMODYNAMIC RELATIONS
The following relationships are obtained from Eqs. (5.22)–(5.25).
(5.26)
(5.27)
(5.28)
(5.29)

## Slide 16
differentiation of which gives
If the partial derivative (6Z/6x)y is itself a function of x and y, being given by (6Z/6x)y=L(x, y), and similarly the partial derivative (6Z/6y)x=M(x, y) then
Thus
and
But, as Z is a state function, the change in Z is independent of the order of differentiation, i.e.,
and hence
(5.30)
Application of Eq. (5.30) to Eqs. (3.12) and (5.10)–(5.12) gives a set of relationships which are known as Maxwell’s equations. These are
112 Introduction to the Thermodynamics of Materials
5.9 MAXWELL’S EQUATIONS
If Z is a state function and x and y are chosen as the independent variables in a closed system of fixed composition then

## Slide 17
Auxiliary Functions 113
(5.31)
(5.32)
(5.33)
(5.34)
Similarly, equations can be obtained by considering variations in composition. The value of the above equations lies in the fact that they contain many experimentally measurable quantities. Consider the dependence of the entropy of an ideal gas on the independent variables T and V, i.e.,
differentiation of which gives
(i)
From combination of the definition of the constant volume heat capacity, Eq. (2.6), and Eq. (3.8) applied to a reversible process conducted at constant volume,
the first partial derivative on the right-hand side of Eq. (i) is obtained as
and the second partial derivative in Eq. (i) is obtained from Maxwell’s equation (5.33). Thus, Eq. (i) can be written as

## Slide 18
114 Introduction to the Thermodynamics of Materials
(ii)
From the ideal gas law,
(iii)
and thus Eq. (ii) can be written as
(iv)
integration of which between the states 1 and 2 gives
(v)
Eq. (v) could have been used for the solution of Ex. 1 presented in Chap. 3, and, for a reversible isentropic process, Eq. (v) collapses to Eq. (2.9).
A similar example of the use of Maxwell’s equations is as follows. For a closed system of fixed composition Eq. (3.12) gives
Thus
Use of Maxwell’s equation (5.33) allows this to be written as
which is an equation of state relating the internal energy, U, of a closed system of fixed composition to the measurable quantities T, V, and P. If the system is 1 mole of ideal gas substitution of Eq. (iii) into Eq. (vi) gives (6U/6V)T=0, which shows that the internal
energy of an ideal gas is independent of the volume of the gas.

## Slide 19
Auxiliary Functions 115
Similarly, for a closed system of fixed composition, Eq. (5.10) gives dH= TdS+VdP in which case
Substituting Maxwell’s equation (5.34) gives
which is an equation of state which gives the dependence of enthalpy on T, P, and V. Again, as the system is an ideal gas, this equation of state shows that the enthalpy of an ideal gas is independent of its pressure.
5.10 THE UPSTAIRS-DOWNSTAIRS-INSIDE-OUT FORMULA
Given three state functions x, y, and z and a closed system of fixed composition, then
or
For an incremental change of state at constant x,
or

## Slide 20
and Eq. (5.12) gives
Therefore, at constant pressure and composition,
or
Dividing throughout by T2 and rearranging gives
which, on comparison with the identity d(x/y)=(y dx–x dy)/y2, shows that
(5.36)
116 Introduction to the Thermodynamics of Materials
This can be written as
(5.35)
Eq. (5.35) can be used with any three state functions and is called the upstairsdownstairs- inside-out formula because each of the state functions appears once in the numerator, once in the denominator, and once outside the bracket.
5.11 THE GIBBS-HELMHOLTZ EQUATION
Eq. (5.2) gives

## Slide 21
Auxiliary Functions 117
Eq. (5.36) is known as the Gibbs-Helmholtz equation and is applicable to a closed system of fixed composition undergoing processes at constant composition. For an isobaric change of state of a closed system of fixed composition, Eq. (5.36) gives the relation of the change in G to the change in H as
(5.36a)
This equation is of particular use in experimental thermodynamics, as it allows OH, the heat of a reaction, to be obtained from a measurement of the variation of OG, the free energy change for the reaction, with temperature, or, conversely, it allows OG to be obtained from a measurement of OH. The usefulness of this equation will be developed in Chap. 10.
The corresponding relationship between A and U is obtained as follows: Eq. (5.1) gives
and manipulation similar to the above gives
(5.37)
This equation is only applicable to closed systems of fixed composition undergoing processes at constant volume and again, for a change of state under these conditions,
(5.37a)
5.12 SUMMARY
The Helmholtz free energy, A, is given by A=U–TS.
The Gibbs free energy, G, is given by G=H–TS.
For a change of state at constant pressure, OH=qp.
In a closed system held at constant T and V, A can only decrease or remain constant. Equilibrium is attained when A achieves its minimum value.
During an isothermal, isobaric process during which no form of work other than P-V work is performed, i.e., w=0, G can only decrease or remain constant. Equilibrium is attained when G reaches its minimum value.

## Slide 22
118 Introduction to the Thermodynamics of Materials
6. Internal energy varies with S, V, and composition as
Enthalpy varies with S, P, and composition as
Helmholtz free energy varies with T, V, and composition as
and Gibbs free energy varies with T, P, and composition as
7. Maxwell’s equations are
With x, y, and z as state functions, the upstairs-downstairs-inside-out formula is

## Slide 23
Auxiliary Functions 119
and
5.13 EXAMPLE OF THE USE OF THE THERMODYNAMIC RELATIONS
Eq. (2.8) gives the relationship between Cp and Cv as
(2.8)
The use of the thermodynamic relations allows the difference between Cp and Cv to be expressed in terms of experimentally measurable quantities. Eq. (5.27) gives
Thus
By definition
9. The Gibbs-Helmholtz equations are

## Slide 24
Maxwell’s equation (5.33) gives
and the upstairs-downstairs-inside-out formula, using P, V, and T, gives
Thus
In Chap. 1, the isobaric thermal expansivity was defined as
Similarly, the isothermal compressibility of a substance, or system, is defined as
which is the fractional decrease in the volume of the system for unit increase in pressure at constant temperature. The negative sign is used to make ß a positive number. Thus
(5.38)
120 Introduction to the Thermodynamics of Materials
Thus

## Slide 25
Auxiliary Functions 121
and the right-hand side of this equation contains only experimentally measurable quantities.
At 20°C aluminum has the following properties:
Cp=24.36 J/mole·K a
=7.05×10–5 K–1 ß
=1.20×10–6 atm–1
density, q=2.70 g/cm3
The atomic weight of aluminum is 26.98, and thus, at 20°C, the molar volume of aluminum, V, is
and thus the difference between Cp and Cv is
The constant volume molar heat capacity of aluminum at 20°C is thus
PROBLEMS
5.1 Show that
5.2 Show that

## Slide 26
5.4 Show that
5.5 Show that
5.6 Show that
5.7 Show that
5.8 Show that
5.9 Show that
122 Introduction to the Thermodynamics of Materials
5.3 Show that

## Slide 27
Auxiliary Functions 123
5.11 Joule and Thomson showed experimentally that when a steady stream of non-ideal gas is passed through a thermally insulated tube, in which is inserted a throttle valve, the temperature of the gas changes and the state of the gas is changed from P1, T1 to
P2, T2. Show that this process is isenthalpic. The change in T is described in terms of the Joule-Thomson coefficient, µj–T, as
Show that
and show that the Joule-Thomson coefficient for an ideal gas is zero.
  Determine the values of OU, OH, OS, OA, and OG for the following processes. (In (c), (d), and (e) show that an absolute value of the entropy is required.)
    The four processes in Prob. 4.1.
    One mole of an ideal gas at the pressure P and the temperature T expands into a vacuum to double its volume.
    The adiabatic expansion of mole of an ideal gas from P1, T1 to P2, T2.
    The expansion of mole of an ideal gas at constant pressure from V1, T1 to V2, T2.
    The expansion of mole of an ideal gas at constant volume from P1, T1 to P2, T2.
5.10 Show that