بسم الله الرحمن الرحيم

Flow up of implementation celli pass play

| Course Instructor | Wassan S. Hussain |
| --- | --- |
| E-mail | wassansuheil@gmail.com |
| Title | Polymers |
| Course Coordinator | Annual |
| Course Objective | a) Studying classification of polymer materials. b) Establish polymerization mechanism c) Studying Molecular structure of polymers, Polymer chain flexibility, Molecular motion. d) Studying Mechanical tests of polymer materials. e) Definition of phenomena of Polymer viscoelasticity. f) Select Free volume theory &Tg Crystallization. g) Specification of Glass, Rubber transition temperature. |
| Course Description | Introduction to polymer science: Chain conformations in polymers, Rubber elasticity Polymer solutions, Amorphous state and glass transition Crystalline state, Molecular structure of polymers, Polymer chain flexibility, Molecular motion and Glass, Rubber transition temperature , Free volume theory &Tg Crystallization, Mechanical tests, Elastic Modulus, Creep and Stress relaxation, Polymer viscoelasticity and modeling. |
| Textbook | Wiley, introduction to polymer science, 2006 Ajayan, P. M., Schadler, L. S., and Braun, P. V., “Nanocomposite Science and Technology”, WILEY-VCH Verlag GmbH & Co. KGaA Pubishing, ISBN: 3- 527-30359-6, Weinheim, (2003). Buzea, C., Ivan. I., Blandino P, and Robbie K., “Nanomaterials and Nanoparticles: Sources and Toxicity”, Biointerphases; Journal for Biophysical Chemistry-Springer, Vol. 2, Issue 4, pp. (MR17 - MR172), (2007). Tarafdar, J.C. and Raliya, R., “The Nanotechnology”, Published by Scientific Publisher (SP), India, (2012). Guozhong Cao, Nano structures and Nano materials: Synthesis, properties and applications - Imperial College press. |
| Course Assessments | Term Tests | Laboratory | Quizzes | Project | Final Exam |
|  | As (40%) | As (0%) | ---- | ---- | As (60%) |
| General Notes | Type here general notes regarding the course |

Course Weekly Outline

| Week | Date | Topes Covered | Lab. Experiment Assignments | Notes |
| --- | --- | --- | --- | --- |
| 1 |  |  |  |  |
| 2 |  |  |  |  |
| 3 |  |  |  |  |
| 4 |  |  |  |  |
| 5 |  |  |  |  |
| 6 |  |  |  |  |
| 7 |  |  |  |  |
| 8 |  |  |  |  |
| 9 |  |  |  |  |
| 10 |  |  |  |  |
| 11 |  |  |  |  |
| 12 |  |  |  |  |
| 13 |  |  |  |  |
| 14 |  |  |  |  |
| 15 |  |  |  |  |
| 16 |  |  |  |  |
| 17 |  |  |  |  |
| 18 |  |  |  |  |
| 19 |  |  |  |  |
| 20 |  |  |  |  |
| 21 |  |  |  |  |
| 22 |  |  |  |  |
| 23 |  |  |  |  |
| 24 |  |  |  |  |
| 25 |  |  |  |  |
| 26 |  |  |  |  |
| 27 |  |  |  |  |
| 28 |  |  |  |  |
| 29 |  |  |  |  |
| 30 |  |  |  |  |
| 31 |  |  |  |  |

INSTRUCTOR Signature:								Dean Signature:

# Text boxes

Republic of Iraq

The Ministry Of Higher Education

& Scientific Research

University: Diyala

College: Engineering

Department: Materials Engineering

Stage: Third

Lecturer name: Wassan S. Hussain

Qualification: Ass. Lect. materials Eng.

Place of work: Materials Eng. Dept.

University: Diyala

College: Engineering

Department: Materials Engineering

Stage: Third

Lecturer name: Wassan S. Hussain

Qualification: Ass. Lect. materials Eng.

Place of work: Materials Eng. Dept.

Republic of Iraq

The Ministry Of Higher Education

& Scientific Research